## Slide 1: Transducer Engagement
Rose Tavary
Sr. Mechanical Engineer

## Slide 2: Objective
Review Interactions Occurring in Solid-Solid Mixing
Influence of Headspace on Mixing Power and Scaling
Transducer transfers energy from one type to another
Bed
Height
Top Transducer
Bottom Transducer
Headspace

## Slide 3: Comparing Elastic vs Inelastic Particles
Elastic Collisions
  Kinetic Energy Transferred Between Colliding Particles
Inelastic Collisions
  Kinetic Energy Transformed By Particles

## Slide 4: Comparing Elastic vs Inelastic Particles
Inelastic Marshmallows
at 90g
Elastic Marshmallows
at 90g

## Slide 5: Dual Transducer Theory
Large Headspace
Reduced Headspace
Elastic Powder RAM Mixing
2.9”
0.5”
.7”
2.7”

## Slide 6: Dual Transducer Theory
Reduced Headspace
Large Headspace
100g RAM Acceleration
100g RAM Acceleration
100g RAM Acceleration
Elastic Powder RAM Mixing
  Solid Particle Collisions are Initiated by the Vessel’s Transducers

## Slide 7: Dual Transducer Theory
Reduced Headspace
Large Headspace
100g RAM Acceleration
100g RAM Acceleration
100g RAM Acceleration
1g Gravity
Elastic Powder RAM Mixing
  Solid Particle Collisions are Initiated by the Vessel’s Transducers

## Slide 8: Dual Transducer Theory
Reduced Headspace
Large Headspace
100g RAM Acceleration
100g RAM Acceleration
100g RAM Acceleration
1g Gravity
Elastic Powder RAM Mixing
  Solid Particle Collisions are Initiated by the Vessel’s Transducers

## Slide 9: Headspace In Practice – Elastic Particles
Engagement with the Second Transducer is Affected by Adjusting Acceleration and Headspace
Chart: Mixing Sugar - 8 oz Vessel
| 0 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
60% Fill | 0 | 24.3543 | 37.6319 | 67.9229 | 107.9072 | 138.1964 | 170.9995 | 214.2107 | 248.9406 | 308.4497
15% Fill | 0 | 19.0355 | 37.4926 | 35.533 | 38.0711 | 35.533 | 38.0711 | 40.6091 | 45.6853 | 63.4518
Reduced
Headspace
Power Density Increase From Engaging Both Transducers
Large
Headspace

## Slide 10: Headspace In Practice – Elastic Particles
Engagement with the Second Transducer is Affected by Adjusting Acceleration and Headspace
Chart: Mixing Sugar - 8 oz Vessel
| 0 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
60% Fill | 0 | 24.3543 | 37.6319 | 67.9229 | 107.9072 | 138.1964 | 170.9995 | 214.2107 | 248.9406 | 308.4497
15% Fill | 0 | 19.0355 | 37.4926 | 35.533 | 38.0711 | 35.533 | 38.0711 | 40.6091 | 45.6853 | 63.4518
Reduced
Headspace
Power Density Increase From Engaging Both Transducers
Large
Headspace

## Slide 11: Headspace In Practice – Elastic Particles
Engagement with the Second Transducer is Affected by Adjusting Acceleration and Headspace
Chart: Mixing Sugar - 8 oz Vessel
| 0 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
60% Fill | 0 | 24.3543 | 37.6319 | 67.9229 | 107.9072 | 138.1964 | 170.9995 | 214.2107 | 248.9406 | 308.4497
15% Fill | 0 | 19.0355 | 37.4926 | 35.533 | 38.0711 | 35.533 | 38.0711 | 40.6091 | 45.6853 | 63.4518
Reduced
Headspace
Power Density Increase From Engaging Both Transducers
Large
Headspace

## Slide 12: Headspace in Practice - Paste
Engagement with the second transducer can be critical to paste mixes

## Slide 13: Increasing Transducer Contact
Reduce Headspace to engage with 2nd transducer
Increasing the Vessel’s Aspect Ratio

## Slide 14: Headspace and Process Scaling
Increasing Transducer contact and Material being mixed

## Slide 15: Continuous Acoustic Mixing
The CAM Stack Construction Reduces Headspace and increases transducer contact by Using Multiple Transducers
Transducers
Transducers
Transducers

## Slide 16: Continuous Acoustic Mixing
The CAM Stack setup is available for both RAM5 and OmniRAM mixers

## Slide 17: Summary
Solid Particle Collision Intensity Increases with Increased Acceleration and Transducer Contact
Headspace Influences Mixing Intensity
  Particles more distance from the transducer see reduced impact forces
  Engaging a second transducer improves mixing performance
CAM Stack is an option for increasing transducer contact for larger mix quantities

## Slide 18: Dual Transducer - Paste